- INTERNATIONAL ELECTROTECHNICAL COMMISSION (IEC) SYSTEM FOR CERTIFICATION TO STANDARDS RELATING TO EQUIPMENT FOR USE IN EXPLOSIVE ATMOSPHERES (IECEx SYSTEM)

TITLE:  Draft Revision of ExTAG Decision Sheet DS 2012/011– Resistance to light of elastomeric materials

- Circulated to: ExTAG – IECEx Testing and Assessment Group

INTRODUCTION

This document, ExTAG/486/CD Draft Revision of ExTAG Decision Sheet DS 2012/011 – Resistance to light of elastomeric materials was prepared by SGS BASEEFA

It is issued for a six week comment period for consideration by ExTAG Members.

Please submit comments using the comments table, a separate document by

2018 01 12  to

Christine Kane

If there are no comments received the document will be forwarded for publication.

Julien Gauthier

Julien Gauthier

ExTAG Secretary

| Address: IECEx Secretariat Level 33 Australia Square 264 George Street Sydney NSW 2000 Australia Web: www.iecex.com | ExTAG Secretary Mr Julien Gauthier LCIE S.A. 33 Avenue du General Leclerc 92260 Fontenay-aux-Roses FRANCE Tel: +33 1 40 95 55 26 Fax: +33 1 40 95 89 37 Email : julien.gauthier@fr.bureauveritas.com |
| --- | --- |

COLLECTION OF IECEx ExTAG DECISIONS

| Standard: IEC 60079-0 (Ed 4) IEC 60079-0 (Ed 5) IEC 60079-0 (Ed 6) | Clause: 26.10.2 26.10.1 26.10.1 | Draft revision 2017-11-23 |
| --- | --- | --- |
| Subject: Resistance to light of elastomeric materials Status of document: Draft revision of DS 2012/011 | Key words: - Non-Metallic - Elastomeric - Resistance to Light - UV Exposure | # Original Date: 2011-08-17 Originator of proposal: Baseefa TC/SC involved: |
| Question The pass/fail criteria of the test for resistance to light is fully defined where test samples can be subjected to a bending strength test in accordance with ISO 179, but it is left to the discretion of the testing laboratory how to define equivalent pass/fail criteria where the ISO 179 test is not appropriate. What are appropriate pass/fail criteria to apply to elastomeric materials? Answer By reference to the ageing test in A.3.3 of IEC 60079-0 (Ed 4), it is concluded that a variation of less than 20% in hardness may be used as the pass criterion for an elastomeric material following the exposure to the UV light source. NOTE: Although the referenced test is specific for elastomeric sealing rings, it is considered to form an appropriate basis for testing all elastomeric parts. The test method is given in ISO 48. Either Method N (samples nominally 9 mm thick) or Method M (samples nominally 2 mm thick) may be used, as the pass criteria are based on a percentage change in the measured value of IRHD. ISO 48 allows samples to be prepared either by slicing or laminating in order to achieve the required thickness, with all samples having upper and lower surfaces flat, smooth and parallel. The face exposed to the UV light source should be a naturally occurring face of the material as used, since the UV light acts on the surface of the material. Further guidance can be found in IEC 60079-0 (Ed 7). |  |  |